## Slide 1: MH&W International Corp
TDK Soft Ferrite
MH&W Powder Cores
Sendust – High Flux - MPP

## Slide 2: TDK Soft Ferrite History
Analog Filters
Data Transmission
Power
EMI / RFI

## Slide 3: Ferrite For Analog Filter Notch - Band Pass
K Material – NiZn
H6x Material – MnZn
Obsolete as of 1995

## Slide 4: Ferrite For Data Transmission
xDSL - T1/E1 T3/E3
  DN40 – Control of THD – EP Cores
  DN70 – Control of THD – EP Cores
Local Area Network
  DN45/DNW45 – Higher DC Saturation Toroids
Pulse Transformer
  H5B2 – Small Toroid - Large Δβ

## Slide 5: Control of THD
Premium Material was Gapped H5C3
DN40 Developed For Low Cost Control of THD
DN70 New Material For the Control of THD

## Slide 6: DN70 Material Characteristics Material Specifications

## Slide 7: DN70 Material Characteristics Initial Permeability μi

## Slide 8: Graph of H5C3 DN40 DN70 vs Temperature

## Slide 9: Graph of H5C3 DN40 DN70 vs Saturation Flux Density

## Slide 10: DN45 Material Characteristics

## Slide 11: DN45 μe vs HDC

## Slide 12: DN45 μe vs Temperature

## Slide 13: TDK Power Ferrite
Material | Initial Perm | Comments |  | Material | Initial Perm | Comments
H7A | 4500 | Obsolete |  | PC45 | 2500 | Optimized 70 – 80 ˚ C
H7B | 3700 | Obsolete |  | PC46 | 3200 | Optimized 40 – 50 ˚ C
PC30 | 2500 | Obsolete (H7C1) |  | PC47 | 2500 | Optimized PC44
PC33 New 2003 | 1400 | Chokes High Bsat |  | PC50 | 1400 | One (1) MHz (H7F)
PC40 | 2300 | (H7C4) |  | PC95 New 2003 | 3300 | Broadband Core Loss
PC44 | 2400 |  |  | DN50 | 5500 | High Perm Room Temp

## Slide 14: PC33 Ferrite Power Material
High DC Saturation 20 – 25% higher
High Core Losses – detriment for transformers
Best Suited For Output Chokes

## Slide 15: PC33 Material Characteristics

## Slide 16: NI Limit vs Al For PC44 & PC33

## Slide 17: PC95 Material
Constant Core Loss Over Temperature
Same Price as Other Core Materials
Replaces PC44 and PC47 in Board Mounted Power (Planar) Designs
Availability Only In Planar Due To Limited Production

## Slide 18: Material Characteristics of PC95 Compared To PC44 PC45 PC46

## Slide 19: Graph of Core Loss vrs Temperature PC44 PC45 PC46 PC95 Typical Value

## Slide 20: Graph of Initial Perm vrs Temperature PC44 PC45 PC46 PC95 Typical Values

## Slide 21: Graph of Bs & Br vrs Temperature PC44 PC45 PC46 PC95 Typical Values

## Slide 22: Graphs of Core Loss & Bs vrs Temperature PC47 PC95

## Slide 23: Shapes For Board Mounted Power
ER and EIR Series
EI Series (EI14, EI18 & EI22)
EER Series
EE Series (EE20/8/8)
PQI16/7.8 (HPQ16/5.4 + PLT16/2.4)
EL/ELT Series

## Slide 24: ER/EIR & EI Shape

## Slide 25: EER & EE Shape

## Slide 26: EL / ELT Shape

## Slide 27: TDK Power Material Selection Guide

## Slide 28: MH&W OEM Powder Core Sendust High Flux MPP
Sendust Toroid – Perm = 26, 60, 75, 90, 125
Sendust EE – Perm = 26, 40, 60
High Flux Toroid – Perm = 26, 60, 125, 147 160
MPP Toroid – Perm = 26, 60, 125, 147, 160, 173, 200
MPP Washer – Perm = 125 and custom

## Slide 29: MH&W Powder Core Selection Guide